## Slide 1: Characterization of the conductive structures in the periplasm of cable bacteria using combined TOF-SIMS/AFM
Raghavendran Thiruvallur Eachambadi, Henricus T.S. Boschker, Valentina Spampinato, Alexis Franquet, Silvia Hidalgo-Martinez, Filip J.R. Meysman, Jean V. Manca
ragha.thiruvallur@uhasselt.be
18.09.2018

## Slide 2: Outline
Why study cable bacteria?
Instrumentation
Results
Cable bacteria model

## Slide 3
Pfeffer, Christian; Larsen, Steffen; Song, Jie; Dong, Mingdong; Besenbacher, Flemming; Meyer, Rikke Louise; Kjeldsen, Kasper Urup; Schreiber, Lars; Gorby, Yuri A.; El-Naggar, Mohamed Y.; Leung, Kar Man; Schramm, Andreas; Risgaard-Petersen, Nils; Nielsen, Lars Peter
SY Malkin et al., 2014
Notes: Indications of LDET: EFM, cutting experiment (Oxygen consumption)

## Slide 4: What are cable bacteria?
Long, unbranched chain of cells: >30 mm and up to 2 x 104 cells
Freshwater/saltwater sediments
Respiration via redox reaction
Electron transport in the range of centimeter
Image courtesy: microbial-electricity.eu
Pfeffer et al. Nature, 2012
Long, unbranched chain of cells: >30 mm and up to 2 x 104 cells
Freshwater/saltwater sediments
Respiration via redox reaction
Electron transport in the range of centimeter

## Slide 5
Electrostatic force microscopy imaging at meeting point of two cells
Pfeffer et al. Nature, 2012
SEM image of a cable bacterium filament
SY Malkin et al. 2014
AFM imaging at junction
R. Cornelissen et al. Manuscript under review

## Slide 6: Typical dimensions of a cable bacteria cell
3.38 µm
3.71 µm
1.13 µm
0.87 µm
4.93 µm
3D view obtained from AFM height image
Fiber-to-fiber distance
180±15 nm
Fiber core
46±6 nm
Fiber shell
117±10 nm
Cross section image from FIB/SEM
R. Cornelissen et al. Manuscript under review
Representative cross-section of a cell body
Extraction procedure

## Slide 7: Objectives
Composition of the conductive structures c.f. fibers using TOF-SIMS/AFM
Develop a model of electron conduction in cable bacteria

## Slide 8: Outline
Why study cable bacteria?
Instrumentation
Results
Cable bacteria model

## Slide 9: Instrumentation
TOF-SIMS V at imec, Belgium
Sputter source: Ar cluster 10 keV (4000 atoms/cluster); Analysis source: Bi3+ at 30 keV
Depth profiles obtained with alternating sputtering and analysis beams; delayed extraction
In-situ AFM used in contact mode
ToF
AFM
Ga FIB
Bi beam
Ar cluster beam
O2, Cs beams
Alexis Franquet
Valentina Spampinato

## Slide 10: Outline
Why study cable bacteria?
Instrumentation
Results
Cable bacteria model

## Slide 11
Ni+
C4H8N+
CH3O+
Depth profiling in positive polarity

## Slide 12
Depth profiling in negative polarity
CN-
HS- , S-
CH3O-
C3H3O2-

## Slide 13: Comparison of depth profiling in both polarities
Chart: Positive
Chart: Negative
H.T.S. Boschker, R. T. Eachambadi et al. Manuscript under preparation
C4H8N+
C3H2N-
CH3O+
Ni+
S-
CH3O-

## Slide 14: ToF-SIMS: 3 most common depth profiles
Nitrogen containing organics:
pos and neg mode  many N and NO containing fragments, characteristic ions of many amino acids (pos mode)
Ni and S:
pos mode  Ni and isotopes
neg mode  S- and isotopes, HS-, C2S-, NaHS-, NaH2S-, C2HS-, CSN-, C3SN-, C2S2-
Oxygen containing organics:
pos mode  CH3+, H3O+, CHO+, CH2O+, CH3O+, C2HO+, C2H2O+, C2H3O+, C2H5O+, C3HO+, C3H5O+, C2H3O2+, C2H4O2+, C3H3O2+, C3H5O2+, CHO2Na2+, C4H2O2Na+
neg mode  CHO-, CH3O-, C2HO-, C2H3O-, CHO2-, C3HO-, CH2ONa-, C3H3O-, C2HO2-, C3H5O-, C2H2O2-, C2H3O2-, C2H4O2-, C4H3O-, C3HO2-, C4H5O-, C3H2O2-, C3H3O2-, C2HO3-, C4H5O2-, C3H2O3-, C3H3O3-, C4H3O3-, C4H5O3- , C4H5O4-, C7H5N2O2-, C5H4N5O-/C4H8NO5-
Protein
Polysaccharides
Organic ligated NiS group
N
C-C-C-S-S-Ni+
H.T.S. Boschker, R. T. Eachambadi et al. Manuscript under preparation

## Slide 15: Calibration of sputter depth with the in-situ AFM
Before Sputter
After sputter
Difference image
Chart: Sputter time (sec)
| 200 | 175 | 59 | 53 | 0
Sputter depth nm | -63.5 | -59 | -21 | -15 | 0
Ni and S
O-org
H.T.S. Boschker, R. T. Eachambadi et al. Manuscript under preparation
N-org

## Slide 16: Outline
Why study cable bacteria?
Instrumentation
Results
Cable bacteria model

## Slide 17: Cable bacteria model
Protein rich fibers (N-organics)
Polysaccharide rich layer that holds the fibers together (O-organics)
Ni and S rich core
ca. 100 nm
H.T.S. Boschker, R. T. Eachambadi et al. Manuscript under preparation

## Slide 18: Hybrid SIMS
Provides high mass resolution (>240k) and mass accuracy (<1 ppm)
Gas cluster imaging
Dual analyser: TOF and Orbitrap
Advantageous in biological samples
Hybrid SIMS: courtesy: iontof.com

## Slide 19: Hybrid-SIMS: Better peak identification
The highly increased mass resolution of Orbitrap-SIMS leads to much better peak identification for organic biological samples (Mz > 75)
ToF-SIMS (Res ~ 6 k)
Orbitrap-SIMS (Res ~300 k)
Si2C2H7- 87.0087
C3H3O3- 87.0082
C2H3SN2- 87.0017
C6HN- 87.0109
C2H3SN2-
C6HN-
C3H3O3-
Si2C2H7-
Intensity (counts)
Intensity (counts)
m/z
m/z
Notes: The main issue was to separate H3H3O3- from C6HN-. Si2C2H7- is also a less likely fragment as it contains Si which is low in the samples. C2H3SN2- is already too far off in ToF-SIMS.

## Slide 20: ThanX for your attention!
Acknowledgements
X-LAB/UHasselt :
R. Bonné, R. Cornelissen, J. L. Hou, J. V. Manca, B. Cleuren, R. Valcke
UAntwerpen :
H. T. S. Boschker, S. Hidalgo-Martinez, J. Geelhoed, F. J. R. Meysman
Imec :
Valentina Spampinato, Alexis Franquet
Funding :
UHasselt and FWO/Hercules

## Slide 21: Why makes cable bacteria interesting?
Abundance in different environments
Electron transport over cm length scale
Potential applications in bio-electronics
Conduction mechanism unknown: Analysis needed
SEM image of a cable bacterium filament

## Slide 22: Sample preparation (extraction treatment)
Washed in MilliQ water
Incubation for 10 min at RT in a 1 % (w/w) aqueous solution of sodium dodecyl sulfate (SDS); wash in MilliQ
Incubation for 10 min at RT in 1 mM aqueous solution of ethylene diamine tetra acetic acid (EDTA), incubated for 10 min at RT
“Extracted” filaments laid on gold sputtered Si substrates
3.05 µm
3.78 µm
0.32 µm
0.12 µm
3.85 µm

## Slide 23: Understanding the structure of Cable bacteria
1 µm
1 µm
R. Cornelissen et al. Manuscript under review
1 µm
Cell junction
Cell body
Focused Ion Beam/Scanning electron microscopy imaging

## Slide 24: Structural composition of cable bacteria
Inner membrane
Fiber (50 nm)
Outer membrane
(4 µm)
Periplasm
Cytoplasm
Ridge segment
Radial connection
Central node
Outer membrane
(4 µm)
Fiber (50 nm)
Cross-section at the cell body
Cell junction
3D representation of cable bacteria
The conductive structures are present in the periplasm!
R. Cornelissen et al. Manuscript under review

## Slide 25: Conductive fibers
1 µm
After extraction treatment
Conducting fiber (50 nm)

## Slide 26: Cable bacteria model
Protein rich fibers
Polysaccharide rich layer that holds the fibers together (peptidoglycan?)
Often only first transition most clearly visible in ToF-SIMS:
Smearing of depth profiles by uneven sputtering with depth
Signal from junctions
Variation in SDS+EDTA extraction efficiency
Ni and S rich core
ca. 100 nm
H.T.S. Boschker, R. T. Eachambadi et al. Manuscript under preparation

## Slide 27: Future work
To use Ar cluster as analysis beam to study higher m/z data
To understand the exact location of elements such as Ni and S using fast imaging techniques
To study electrical properties such as conductivity and relative permittivity using the in-situ AFM

## Slide 28: Depth profiling in negative polarity
All N-organics
All O-organics
H.T.S. Boschker, R. T. Eachambadi et al. Manuscript under preparation

## Slide 30: Typical dimensions of a cable bacteria cell
3.38 µm
3.71 µm
1.13 µm
0.87 µm
4.93 µm
3D view obtained from AFM height image
Fiber-to-fiber distance
180±15 nm
Fiber core
46±6 nm
Fiber shell
117±10 nm
Cross section image from FIB/SEM
R. Cornelissen et al. Manuscript under review

## Slide 31: Comparisons of depth profiling in both polarities
H.T.S. Boschker, R. T. Eachambadi et al. Manuscript under preparation
Sputter time (sec)
Normalized counts
Sputter time (sec)