Hydrogenation of Diamond Nanowire Surfaces for Effective Electrostatic Charge Storage

Kalpataru Pandaa,b,*, Jae-Eun Kima, Kamatchi Jothiramalingam Sankaranc, I-Nan Lind, Ken Haenene,f, Georg S. Duesbergb, Jeong Young Parka,g*

aGraduate School of EEWS and Department of Chemistry, Korea Advanced Institute of Science and Technology (KAIST), Daejeon, 34141, South Korea

bInstitute of Physics, EIT 2, Faculty of Electrical Engineering and Information Technology, Universität der Bundeswehr München, Werner-Heisenberg-Weg 39, 85577 Neubiberg, Germany

cCSIR-Institute of Minerals and Materials Technology, Bhubaneswar-751013, Odisha, India

dDepartment of Physics, Tamkang University, 251 Tamsui, Taiwan, Republic of China

eInstitute for Materials Research (IMO), Hasselt University, 3590 Diepenbeek, Belgium

fIMOMEC, IMEC vzw, 3590 Diepenbeek, Belgium

gCenter for Nanomaterials and Chemical Reactions, Institute for Basic Science (IBS), Daejeon, 34141, South Korea

Figure S1. XPS spectra of (i) pristine and (ii, iii, iv) H2 plasma-treated DNW films for (ii) 5, (iii) 10, and (iv) 15 min. The data are fitted to Lorentzian peaks with binding energies at 284.1, 285.2 and 286.0 eV corresponding to sp2 C=C, sp3 C–C and C=N bonding and their relative intensities are tabulated in Table I. In the DNW0 film, the sp3 C–C bonding is predominant with a peak intensity of 50.7%, while the sp2 C=C peak intensity is 40.9% (curve i, Figure S1). The C=N peak is seen with an intensity of 8.4% at a binding energy of 286 eV. The appearance of C=N is not surprising because the films were grown in a N2 containing plasma. A significant increase in the sp2 phase fraction is observed, which is caused by the H2 plasma treatment (i.e., the sp2 C=C peak intensity increases to 48.1% for the DNW5 films (curve ii, Figure S1) and to 63.9% for the DNW10 films (curve iii, Figure S1)). However, extended H2 plasma treatment removes the graphitic phase content from the surface (curve iv, Figure S1) thereby decreasing the sp2 phase fraction to 35.9%.

Table I. Relative intensities of the various components of the C1s XPS spectra from the pristine DNW0 and the H2 plasma-treated DNW films.

| Peak position (eV) | Chemical bond | Peak intensity (%) |
| --- | --- | --- |
|  |  | DNW0 | DNW5 | DNW10 | DNW15 |
| 284.1 | sp2 C=C | 40.9 | 48.1 | 63.9 | 35.9 |
| 285.2 | sp3 C–C | 50.7 | 40.1 | 29.2 | 58.9 |
| 286.0 | C=N | 8.4 | 11.8 | 6.9 | 5.2 |

Figure S2. FESEM images of the diamond-coated Si tip (a) before and (b) after the load-dependent charge storage experiments on the DNW surface where the same tip was used many times. This indicates that the diamond-coated Si tips are stiff enough and did not change size because of the high load. Even a high bias of ±10 V did not change the tip.

Figure S3. (a) Surface topography of the DNW10 surface that was written with a tip bias of −1 V in the marked square. (b) The corresponding KPFM potential signal clearly shows a negative potential shift. After reversing the tip polarity to +1 V, the same area was written again (all other parameters were the same as the first writing procedure at −1 V). (c) After the writing process at +1 V, the corresponding KPFM potential signal at the same position shows that the trapped charge can be erased by applying an exact opposite bias to the AFM tip. This indicates that the DNW surface can be rewritten. It is noted that there is still a small residual charge left on the writing area. Image sizes: (a, b, c) 4 µm.