## Slide 1
October 9 2024 – Honolulu, HI, USA
Dries De Sloovere
Improving the Electrochemical Stability of Lithium‐Rich Cobalt‐Free Layered Oxides for Lithium‐Ion Batteries By Phase Engineering

## Slide 2: Introduction
Why Co-free?
LIB technology for consumer EVs is dominated by cobalt-containing LiNixMnyCozO2 chemistry.
Large reliance on Co:
High cost
Scarcity
Vulnerable global supply chain
Toxicity
Growing consensus to eliminate cobalt in high-energy-density cathode materials.
De Sloovere et al. Small, 2024.

## Slide 4: Introduction
Which material class?
Xiang et al. Adv Mater, 2022.

## Slide 5: Introduction
Which material class?
Xiang et al. Adv Mater, 2022.
NMC

## Slide 6: Introduction
Which material class?
Xiang et al. Adv Mater, 2022.
NMC
LiFePO4

## Slide 7: Introduction
Which material class?
Xiang et al. Adv Mater, 2022.
NMC
LiFePO4
Lithium-rich layered oxides

## Slide 8: Li-rich layered oxides
Combination of:
LiMO2, rhombohedral
Lower capacity
TM redox
Li2MnO3, monoclinic
Higher capacity
TM redox
Oxygen redox
Li et al., Chem Sov Rev, 2019.

## Slide 9: Synthesis

## Slide 10: Synthesis
Sample | Nominal composition
LNMA0 | Li1.26Ni0.15Mn0.61O2
LNMA1 | Li1.26Ni0.15Mn0.60Al0.01O2
LNMA5 | Li1.26Ni0.15Mn0.56Al0.05O2
LNMA10 | Li1.26Ni0.15Mn0.51Al0.1O2
Cobalt-free
Large Li excess
Increasing amount of Al

## Slide 11: Electrochemical performance
Decrease in initial discharge capacity
Increase in capacity retention
Decrease in voltage fade
Can we figure out why Al doping improves the electrochemical stability?

## Slide 12: POWDER CHARACTERISATION
AN INCOMPLETE IMAGE

## Slide 13: X-ray diffraction
Materials are phase-pure
Data can be modeled as either a combination of rhombohedral and monoclinic phases, or as a monoclinic phase.
Rhombohedral and/or monoclinic?
(003)R
(001)M
(020)M
(101)R
(111)M
(104)R
(131)M
Si
Si
Si

## Slide 14: Raman spectroscopy
Decrease in A1g peak corroborates Al incorporation
~560 cm-1: Al promotes formation of R phase
Incorporating more Al increases the rhombohedral character of the samples.
Rhombohedral and/or monoclinic?

## Slide 15: NMR spectroscopy
Increasing the extent of Al doping increases the amount of the rhombohedral phase in the samples.
7Li and 6Li NMR

## Slide 16
Why is the stability improved?

## Slide 17: POST MORTEM CHARACTERISATION
SHEDDING LIGHT ON DEGRADATION

## Slide 18: Raman spectroscopy
Formation of a disordered spinel as degradation phase
Low capacity
Doesn’t allow to quantitatively study the effect of doping
Undoped
Doped

## Slide 19: Hypermodel data fusion
An advanced TEM technique
Statistical technique (principle component analysis) allows to identify phases within the sample based on spectroscopy information
This allows to make abundance maps: location of the phases
Quantitative: fractional phase abundance
Thersleff & Tai, 2023.

## Slide 20: Hypermodel data fusion
“
“
Three phases were identified:
Monoclinic phase
Rhombohedral phase
Disordered spinel

## Slide 21: Hypermodel data fusion
“
“
“
“
Monoclinic phase
Rhombohedral phase
Disordered spinel

## Slide 22: Hypermodel data fusion
“
“
“
“
“
Monoclinic phase
Rhombohedral phase
Disordered spinel

## Slide 23: CONCLUSION

## Slide 25: Acknowledgements
Satish Kumar Mylavarapu, Jan D’haen, Thomas Thersleff , Aleksander Jaworski, Jekabs Grins, Gunnar Svensson, Radostina Stoyanova, Leif Olav Jøsang, Kunkanadu Rajappa Prakasha, Maximiliano Merlo, Elías Martínez, Marc Nel‐lo Pascual, Jordi Jacas Biendicho, Marlies K. Van Bael, An Hardy,
This project has received funding from the European Union’s Horizon 2020 research and innovation programme under grant agreement No 875568

## Slide 26
October 9 2024 – Honolulu, HI, USA
Dries De Sloovere
Improving the Electrochemical Stability of Lithium‐Rich Cobalt‐Free Layered Oxides for Lithium‐Ion Batteries By Phase Engineering